## Slide 1: Lattice Parameter Changes of Binary Alloys
CME 502 Final Presentation
Melanie Brito

## Slide 2: Background 02 04 01 Goals Bulk and Shear Moduli 03 Composition Effects Grain Size Effects 05 Curve Fitting 08 Table of contents
Intro to the FeMg system
Goal of the Python Code
06
Grain Boundary Segregation
07
Plotting

## Slide 3: Background 01
Introduction to the FeMg system

## Slide 4: Fe Mg ODS Alloys
PI: Dr. Jason Trelewicz
Project: Mechanical Ball Milling of Iron Magnesium powders to make ODS alloys
Goal: To make an oxide dispersion strengthened (ODS) alloy of Fe and Mg.
What is an ODS alloy?
  When 2 powders are milled together, the solute phase becomes dispersed and upon annealing, forms oxide deposits throughout the material.
  Beneficial because gives the alloy enhanced properties at elevated temperatures.
    Ideal for fusion reactors.
ODS alloys successfully made for many systems but rarely for FeMg due to problems with Fe oxidation.

## Slide 5: Fe Mg Milling
Experimental: Different compositions of FexMg alloys milled at the same conditions.
  x represents 0.01, 0.05, 0.10, 0.15, 0.20 at% Mg
  PM 100 Ball Mill (500 RPM, 10 hours, 3.5wt% ethanol PCA)
Fe Mg solid solution is made where BCC Mg becomes incorporated into the BCC Fe lattice.
  Mg usually HCP lattice stable but shifts to BCC.
Some Mg segregates to the grain boundaries.
  It is desired to know the extent of this process/ how much Mg is in the grain boundaries.
HCP Mg
BCC Mg
Materials Project
Notes: https://materialsproject.org/materials/mp-153
https://materialsproject.org/materials/mp-13

## Slide 6: Fe Mg Properties
XRD patterns of the different samples were taken and Reitveld Refinements used to get Lattice Parameter and Grain Size.
Mg segregation to the grain boundary causes changes in the lattice parameter from BCC Fe literature value.
  Increasing changes as composition changes.
TEM Image of Fe15Mg powder
XRD Pattern Refinement (Fe15Mg)

## Slide 7: Lattice Parameter Changes
Want to determine what physical phenomena cause lattice parameter shifts and to what extent.
Changes can be broken down into several effects
  Compositional Effects
    Mg compositons change LP
  Grain Size Effects
    Milling changes grain size → changes LP
  Grain Boundary Segregation
    Amount of Mg in GB → changes LP
Crystal Structure Overview
Notes: https://study.com/learn/lesson/cubic-unit-cell-lattice-parameter-crystal-structure.html

## Slide 8: Goals 02
Goal of the Python Code

## Slide 9: Lattice Parameter Calculations
There are detailed equations to calculate the LP changes due to each one of the effects.
Many parts of the equations need to be changed for each of the different compositions and this can be time consuming and leave room for errors and typos.
Solution: Use loops and arrays to manipulate the equations to get the lattice parameter changes for each of the compositions
Each one of the compositions will have
  Δacomp ,ΔaGS , ΔaGBS (lattice parameter changes)
  alit, aexp (literature and experimental LP)

## Slide 10: Lattice Parameter Calculations
Composition Effects
Grain Size Effects
Grain Boundary Segregation
Lubarda et al.
Rane et al.

## Slide 11: Plotting and Curve Fitting
Plot of Lattice Parameter (A) vs Composition (at% Mg) made to compare the effects
  Experimental
  Vegard’s Law
  Composition Effects
  Grain Size Effects
  Grain Boundary Segregation
Curve fitting will be used on the experimental data to get an equation for lattice parameter as a function of composition.
Linear Regression Model will be used for the curve fitting (linregress)
Curvefit function will also be used (linear fit, 2nd order, 3rd order)
Notes: https://materialsproject.org/materials/mp-153
https://materialsproject.org/materials/mp-13

## Slide 12: Effective Bulk and Shear Moduli 03

## Slide 13: Effective Bulk and Shear Modulus
Formulas for effective shear modulus uses bulk and shear moduli for each of the pure components (BCC Fe and BCC Mg).
  Values obtained from literature (Lubarda et al.)
Solve for the value of shear modulus (μ) and use this to solve for bulk modulus (k)
  Must be repeated for each composition (x)
  All values in GPa.
Lubarda et al.

## Slide 14: Outline of Code For loop over compositons (x)
Make arrays for the bulk and shear moduli for the pure components (kpure, upure) and different Mg compositions (x)
Pre-allocate arrays for effective moduli (eu, ek)
Define functions for the equations for effective moduli (efshear, efbulk)
While loop that runs over potential values of μ
Plug potential shear modulus values (start with 50 GPa) into the function (efshear) and when output changes from positive to negative (μ goes through 0) save the μ value and break the loop.
Find the effective bulk modulus (K)
Save effective moduli values to a text file

## Slide 16: Output in Text file
As Mg increases, moduli become closer to the Mg moduli values.

## Slide 17: Composition Effects 04

## Slide 18: Composition Effects
Lattice parameter from composition effects calculated using an elasticity inclusion model and size of solute in solvent matrix (Lubarda et al.)
Must be repeated for each composition (x)
Lattice parameter change due to composition effects also calculated
All values in Angstrom

## Slide 19: Composition Effects
a1= LP from literature
R1= Seitz Atomic radius (BCC Fe)
k= number of atoms per unit lattice cell (2 for BCC)
x= Mg concentration
ϑ= Crystal structure of lattice (1 for BCC)
γ ,γ1, γ2= Having to do with bulk and shear moduli of pure components
C= Relation between Seitz radius and γ2
Lubarda et al.

## Slide 20: Outline of Code For loop over compositons (x)
Make array for alit , literature values for the LP of BCC Fe and BCC Mg
Pre-allocate arrays for γ, acomp and Δacomp
Find γ
Save acomp and Δacomp values to a text file
Make variables for k, ϑ, γ1, γ2, R1, C
Calculate acomp and Δacomp

## Slide 22: Output in Text file
Increasing Mg causes an increase in the lattice parameter.

## Slide 23: Grain Size Effects 05

## Slide 24: Interfacial Stress
Interfacial stress leads to hydrostatic compression and this causes the lattice to shrink.
σs: Interfacial stress (Rane et al.)
D: crystallite size as determined by XRD Reitveld refinement
a0: LP due to composition effects
K: Effective bulk modulus
Rane et al.

## Slide 25: Excess Free Volume
Nanocrystalline materials have highly disordered grain boundaries.
  Leads to defects and vacancies and therefore excess free volume.
a0: LP due to composition effects
D: crystallite size as determined by XRD Reitveld refinement
ξ: Grain boundary thickness (estimated 1 nm)
Rane et al.

## Slide 26: Grain Size Effects
Lattice Parameter due to grain size effects is the sum of the interfacial stress and excess free volume.
ΔaGS in nanometers.
Must be repeated for each composition (x).

## Slide 27: Outline of Code For loop over compositons (x)
Make variables for σs and ξ
Pre-allocate arrays for Δais , ΔaEFV , ΔaGS and divide acomp by 10
Calculate Δais
Save Δais , ΔaEFV , and ΔaGS values to a text file
Make an array for experimental grain size values (d)
Add Δais and ΔaEFV
Calculate ΔaEFV

## Slide 29: Output in Text file
Interfacial stress shrinks the lattice with increasing Mg while EFV expands it.

## Slide 30: Grain Boundary Segregation 06

## Slide 31: Grain Boundary Segregation
Lattice Parameter change due to grain boundary segregation is calculated as the difference between the experimental and literature values for BCC Fe LP minus the changes due to the other effects.
Must be repeated for each composition (x)
All values in Angstrom

## Slide 32: Outline of Code For loop over compositons (x)
Make an array for the experimental lattice parameter values, aexp.
Pre-allocate an array for ΔaGBS
Calculate ΔaGBS by indexing into arrays for ΔaGS , Δacomp, alit, and aexp.
Save ΔaGS , Δacomp, ΔaGBS , alit, and aexp. values to a text file

## Slide 34: Output in Text file
Increased Mg causes more grain boundary segregation and shrinking lattice parameter.

## Slide 35: Plotting 07

## Slide 36: Plotting
Lattice Parameter (A) vs Mg Composition (at%) Plot made.
  Experimental
  Vegard’s Law
    Simplified way to account for compositional effects for binary alloys
  Composition Effects
  Grain Size Effects
  Grain Boundary Segregation
Dane et al.

## Slide 37
Compositional effects expand the lattice.
Grain boundary segregation shrinks the lattice.

## Slide 38: Curve Fitting 08

## Slide 39: Curve Fitting
It is desired to find a simplified function for the relationship between Lattice Parameter and Mg composition.
  Can be used for quick estimates of the lattice parameter for intermediate compositions.
As seen from plot, should be a linear trend between the 2 parameters.
  Linear Regression Model (Least Squared Method) (linregress)
  Curve_fit Function with a linear function
  Find R2 and RMS Error for both methods
Plot the 2 fits and the experimental data to see how it compares.

## Slide 40: Outline of Code
Import stats from scipy
Call the linregress function
Print the output equation
Find R2 and RMS
Import curve_fit function
Define linear function
Call curve_fit function
Print the output equation
Find R2 and RMS
Plot the experimental data and the fitted lines.

## Slide 43: Curve Fitting
Linear function does not seem to be a good fit.
Curvefit function can be used to fit higher order polynomials.
Experimental data should be linear but it is worth trying different types of fits to see the result.
2nd and 3rd order polynomial fits are done
  R2 and RMS error found.
  Fits plotted with experimental data.

## Slide 46: Conclusion and Future Work

## Slide 47: Conclusion and Future
Pyhton3 code was used to get the lattice parameter changes due to changing Mg compostions in FeMg ODS alloys.
Several physical phenomena make contributions to the changes.
  Some expand the lattice, some cause it to shrink.
Linear regression and curve fitting (1st, 2nd, 3rd order) were used to get a simplified trend of LP and composition.
  Once more accurate experimental data is gathered, the fits will be better.
Python code allowed for quicker calculations with no errors and publication ready plots.
Future work includes better experimental data and creating a data class/library with functions for the calculations.

## Slide 48: Sources
“MP-13: Fe (Cubic, Im-3M, 229).” Materials Project, https://materialsproject.org/materials/mp-13.
“MP-13: Fe (Cubic, Im-3M, 229).” Materials Project, https://materialsproject.org/materials/mp-13.
Codoluto, Daniel. “Crystal Structure Overview.” Study.com, https://study.com/learn/lesson/cubic-unit-cell-lattice-parameter-crystal-structure.html.
Lubarda, V.A. “On the Effective Lattice Parameter of Binary Alloys.” Mechanics of Materials, vol. 35, no. 1-2, 2003, pp. 53–68., https://doi.org/10.1016/s0167-6636(02)00196-5.
Rane, Gayatri Koyar, et al. “Non-Monotonic Lattice Parameter Variation with Crystallite Size in Nanocrystalline Solids.” Acta Materialia, vol. 61, no. 12, 2013, pp. 4524–4533., https://doi.org/10.1016/j.actamat.2013.04.021.
Denton, A. R., and N. W. Ashcroft. “Vegard’s Law.” Physical Review A, vol. 43, no. 6, 1991, pp. 3161–3164., https://doi.org/10.1103/physreva.43.3161.

## Slide 49: Questions?