## Slide 1: Applications of Python Programming for Catalyst Characterization
By: Jamie DeCoster

## Slide 2: Introduction: Research Topic
Automobiles and other combustion sources release carbon monoxide [1,2]
  Oxidizing CO into CO2 reduces toxicity [1,2]
  Platinum group metals are currently used for CO oxidation, but these catalysts are expensive, difficult to obtain and have low activity at low temperatures [3]
Cerium oxide (CeO2) is a promising catalyst as it can easily switch between 4+ and 3+ oxidation states forming oxygen vacancies [4,5,6]
Oxygen vacancies and defect sites are related to catalytic performance as they can act as active sites for CO oxidation
Research examining influence of pretreatment temperature and condition (reducing/oxidizing/inert) on ceria to evaluate the impact on the physiochemical properties and catalytic activity
CeO2
O
O
O
O
CeO2-x
O
O
O
Ce3+
Ce3+
CO
CO2

## Slide 3: The Problem
Characterization of catalysts uses many different techniques
  XRD
  BET
These techniques require various numerical methods to analyze the results
With multiple samples, analysis could take a long time when performed by hand
Many applications capable of the calculations such as OriginLab require subscriptions
[7]
[8]

## Slide 4: Background: XRD
Characterization technique used for determining phase composition, crystal structure, crystallite size, orientation of powder, etc. [10]
Crystallite size requires the use of the Scherrer Equation
Requires determination of
  Maximum value
  2θ value at which the maximum occurs
  Determination of the width of half the maximum
Goal: Plot the XRD spectra and determine the crystallite size
Scherrer Equation [9]
K: Shape Factor λ: X-ray Wavelength
β: FWHM θ: Bragg Angle
[9]

## Slide 5: Background: Brunauer-Emmett-Teller (BET) Analysis
Characterization technique used for determining the specific surface area (SSA), and pore size distributions of catalysts [12]
To determine the SSA, the data must be examined when only a monolayer has formed. (0.025 < P/P0 < 0.30) [12]
Goal: Create a program that can plot adsorption isotherms and calculate the SSA
BET equation
BET equation linearized
Slope= y-intercept=
Monolayer Capacity
: Cross-sectional area of N2 (16.2 Å2)
11

## Slide 6: Background: Brunauer-Emmett-Teller (BET) Analysis
Characterization technique used for determining the specific surface area (SSA), and pore size distributions of catalysts
To determine the SSA, the data must be examined when only a monolayer has formed. (0.025 < P/P0 < 0.30)
BET equation
BET equation linearized
Slope= y-intercept=
Monolayer Capacity
: Cross-sectional area of N2 (16.2 Å2)

## Slide 7: Approach: XRD
Function 1: XRD_import
  1 input: data file name
  Uses pandas to import the data and store it in numpy arrays
  Based on the minimum, shifts all the data to positive intensity values if necessary
  Plots the XRD results

## Slide 8: Approach: XRD
Function 2: XRD_Slice
  5 inputs: 2θ (x) and intensity data (y), value of the peak of interest (optional), spread of peak of interest (optional), and a variable to toggle saving the figure
  Iterates through the data and saves the data within the given range into new x and y arrays
  Displays the plot so user can determine if the peak was properly sliced
  Option to save the figure

## Slide 9: Approach: XRD
Function 3: XRD_FWHM
  2 inputs: 2θ data of the specific peak, and the corresponding intensity data
  Uses curve fitting of a Gaussian function to the data and calculates arrays of data using the fitted-function
  Finds the index of the maximum intensity value and stores the theta location and half max.
2θmax
yhalf-max

## Slide 10: Approach: XRD
Function 3: XRD_FWHM
  Iterates through the data from the maximum in both the +x and –x directions to find two data points that surround half of the maximum.
  Uses interpolation to get the actual 2θ location of the half max
  Subtracts them to get the width at half the maximum (FWHM)
  2 outputs: FWHM and 2θ value of the maximum

## Slide 11: Approach: XRD
Function 4: Scherrer
  4 inputs: FWHM, theta value of the maximum, shape factor (k) (optional) and lamda (optional)
  Plugs the 4 inputs into the Scherrer equation and returns the crystallite size
Scherrer Equation

## Slide 12: Approach: BET
Function 1: N2ads
  1 input: Filename
  Uses Pandas to read the data within the file (for any number of samples)
    Store the column titles
    Iterate through the column titles to index into the data and store it as numpy arrays for any number of samples
  Plots the N2-Adsorption Isotherms
  Returns P/P0 and Vadsorbed

## Slide 13: Approach: BET
Function 2: SSA
  3 Inputs: P/P0 , V, and σ0 (=16.2e-20, optional)
  Creates data in range of 0.025 to 0.3 to be used for the fit
  Uses linear regression of vs.
  Calculates monolayer capacity ( )
  Calculates

## Slide 14: Approach: BET
Script:
  Calls the first function to extract the data
  Open a file to write the specific surface area results to
  Loop through the number of samples and call the second function for each
  Store the data in a numpy array and write to text file

## Slide 15: Results and Discussion: XRD
XRD plots are important for a qualitative analysis of crystallinity (sharp peaks mean more crystalline while broad peaks are more amorphous)
The R2 value was very close to 1 showing that the fitting used for calculating crystallite size is reliable

## Slide 16: Results and Discussion: XRD
The crystallite size remained relatively close at low temperatures (400-500°C).
With increasing calcination temperature (from 500°C to 700°C), the crystallite size decreased
  Shows signs of sintering in the materials elevated temperatures under an oxidizing atmosphere leads to agglomeration of particles and larger crystallites
Sample | Crystallite Size (nm)
Sample 1 (400°C Calcined) | 5.15
Sample 2 (500°C Calcined) | 4.89
Sample 3 (700°C Calcined) | 7.28

## Slide 17: Results and Discussion: BET
Results of Function 1
400°C and 500°C sample exhibit a type IV isotherm with an H1 hysteresis loop. [12]
  Mesoporous structure with well-defined cylindrical pores
700°C sample exhibits a type V isotherm with an H3 hysteresis loop. [12]
  Porous structure with slit shaped pores

## Slide 18: Results and Discussion: BET
Results of Function 1 and 2 and script
The R2 value was very close to 1 showing that the monolayer capacity result is reliable
SSA decreased with increasing calcination temperature (from 500°C to 700°C)
  Shows signs of sintering in the materials elevated temperatures under an oxidizing atmosphere leads to agglomeration of particles and less reactive surface area
Sample | Specific Surface Area (m2/g)
Sample 1 (400°C Calcined) | 219.53
Sample 2 (500°C Calcined) | 204.53
Sample 3 (700°C Calcined) | 83.79

## Slide 19: Conclusions
Utilization of Python allows for an open-source and free method of analyzing large quantities of data.
Calculations of SSA from characterization data can be performed for multiple samples at once thus saving time.
Calculations of crystallite size can be performed using a variety of peaks and can also be used for plotting applications.
The nature of this code allows for a user to easily plug in the data file name and to have the results returned without requiring a significant understanding of Python.
Future work: Creating a user interface using prompts and XRD code working with multiple samples

## Slide 20: References
[1] J.A. Rodriguez et al., Ceria-Based Model Catalysts: Fundamental Studies on the Importance of the Metal-Ceria Interface in CO Oxidation, the Water-Gas Shift, CO2 Hydrogenation, and Methane and Alcohol Reforming, Chem. Soc. Rev. 46 (2017) 1824-1841. https://doi.org/10.1039/C6CS00863A
[2] NASA Global Climate Change, Fourteen years of carbon monoxide from MOPITT. https://climate.nasa.gov/news/2291/fourteen-years-of-carbon-monoxide-from-mopitt/, 2015.
[3] I. Langmuir, The mechanism of the catalytic action of platinum in the reactions 2CO + O2 = 2CO2 and 2H2 + O2 = 2H2O, Transactions of the Faraday Society. 17 (1922) 621-654. https://doi.org/10.1039/TF9221700621.
[4] E. Özkan et al., Rational Synthesis Concept for Cerium Oxide Nanoparticles: On the Impact of Particle Size on the Oxygen Storage Capacity, The Journal of Physical Chemistry C. 124 (2020) 8736-8748. https://doi.org/10.1021/acs.jpcc.0c00010.
[5] E. Aneggi et al., Surface-structure sensitivity of CO Oxidation Over Polycrystalline Ceria Powders, Journal of Catalysis. 234 (2005) 88-95. https://doi:10.1016/j.jcat.2005.06.008.
[6] J. Kullgren, Oxygen Vacancy Chemistry in Ceria, Digital Comprehensive Summaries of Uppsala Dissertations from the Faculty of Science and Technology. 896 (2012) 59.
[7] A. Alshammari et al., Supported Gold Nanoparticles as Promising Catalysts, Catalystic Application of Nano-Gold Catalysts (2016). http://dx.doi.org/10.5772/64394
[8] Origin. Software Cientifico. Software Cientifico S.L. http://www.softwarecientifico.com/origin/
[9] XRD Crystallite (Grain) Size Calculator (Scherrer Equation). Instanano. Instanano. https://instanano.com/all/characterization/xrd/crystallite-size/.
[10] C.F. Holder et al., Tutorial on Powder X-ray Diffraction for Characterizing Nanoscale Materials, ACS Nano 13 (2019) 7359-7365. http://dx.doi.org/10.1021/acsnano.9b05157
[11] Particle Tech Labs, BET Specific Surface Area. https://particletechlabs.com/analytical-testing/bet-specific-surface-area/
[12] M. Thommes et al. Physisorption of gases, with special reference to the evaluation of surface area and pore size distribution, Pure Applied Chemistry. 87 (2015) 1051-1069.