## Slide 1
Fe-MOR Catalysts and Their Performances
for CH4 Oxidation with N2O
CME502
Presenter: Shenglai Li
Instructor: Nav Nidhi Rajput
05/04/2023
Shenglai.Li@stonybrook.edu, Department of Materials Science
and Chemical Engineering, Stony Brook University

## Slide 2
Introduction
Results and Discussion
Conclusion
Experimental and Programming
3
4
2
1

## Slide 3
Science, 2017, 356: 523-527.

## Slide 4
Air 150 ℃
x hours
Air 500 ℃
4 hours
Fe-MOR calcination conditions[1][2]
N2 900 ℃
1 hours
[1] Journal of Catalysis , 2009 , 264 : 163-174.
[2] Chemistry - A European Journal , 2007 , 13 : 7890 -7899.
Ferrocene
Mordenite
Solid state ion exchange

## Slide 5
CH4 + N2O → CH3OH + N2
Theoretical
4CH4 + 4N2O → 2CH3OH + 2CH3OCH3 + HCHO
+ 4N2 + 3O2 + 2H2O + 2CO + 2 CO2
Experimental

## Slide 6
dH = n Cp,m dT
dS = n Cp,m/T dT
△rGm(T) = △rHm(T) – T △rSm(T)

## Slide 7
XRD

## Slide 8
UV-Vis

## Slide 9
Fig. 1 Enthalpy change and Gibbs free energy change with temperature
Reaction is feasible
Exothermic

## Slide 10
Catalyst | Si/Al | Fe /(wt.%) | BET Surface Area/(m2/g)
Fe-MOR-0.1 | 24.8 | 0.09 | 376.8
Fe-MOR-0.5 | 24.3 | 0.48 | 370.4
Fe-MOR-1 | 24.7 | 0.93 | 347.5
Fe-MOR-2 | 24.3 | 1.92 | 314.7
Fe-MOR-3 | 24.5 | 2.88 | 278.3
Table 1 Physical properties of Fe-MOR catalysts
Fe-MOR-0.1, where 0.1 means that the Fe loading is 0.1%, and so on.
Fe loading ≥ 1%, the specific surface area decreases.

## Slide 11
Fig. 2 XRD patterns for MOR and the Fe-MOR catalyst
MOR
Fe-MOR

## Slide 12
Fig. 3 UV-Vis images for MOR and the Fe-MOR catalyst
MOR
Fe-MOR

## Slide 14
Catalyst | Average conversion /(%) |  |  | Selectivity / (%) |  |  |  |  |  |  |  | 
 | CH4 | N2O |  | CH3OH | HCHO | CH3OCH3 | Total oxy- genates | COx |  |  |  | 
Fe-MOR-0.1 | 0.3 | 1.1 |  | - | - | 31.4 | 31.4 |  | 68.6 |  |  | 
Fe-MOR-0.5 | 0.8 | 2.1 |  | 14.3 | 13.8 | 10.2 | 38.3 |  | 61.6 |  |  | 
Fe-MOR-1 | 0.9 | 2.5 |  | 11.8 | 17.4 | 6.8 | 36.0 |  | 64.0 |  |  | 
Fe-MOR-2 | 0.8 | 2.2 |  | 12.2 | 10.1 | 7.5 | 29.8 |  | 69.8 |  |  | 
Fe-MOR-3 | 0.8 | 2.5 |  | 11.1 | 13.8 | 2.8 | 26.7 |  | 73.3 |  |  | 
Table 2 Performances of Fe-MOR-catalysts for CH4 Oxidation with N2O

## Slide 15
High temperature calcination did not destroy the basic structure of Fe-MOR catalysts.
The specific surface area of the catalyst gradually decreased with increasing loading Fe content.
The selectivity and yield of oxygenated organics increased with increasing loading Fe content and then decreased.
Fe-MOR-0.5 catalyst was more effective with a total selectivity of 38.4% for oxygenated organics.
Conclusion

## Slide 16
Thank you.
Any questions, comments, and suggestions?